Vibration Analysis of Functionally graded rotating plate

Mukesh Kumar, Aditya Prakash Yadav

Indian School of Mines Dhanbad

ABSTRACT

The aim of this paper is to investigate three-dimensional vibration analysis of functionally graded rotating annular plates with different boundary conditions. The governing differential equation for the system is derived and the solution to the nonlinear set of equations is generated by implementing a substitution technique. The results of the nonlinear analysis are plotted as characteristics curve i.e. non dimensional frequency response curve for different classical flexural boundary conditions with different variation of material and geometric parameters. Here volume fraction of material plays an important role for becoming anisotropic of the material. For each boundary condition, variation of material properties (i.e. elastic modulus & density) in the thickness direction of the plate is considered. In the present study, a detailed work has been carried out to develop a finite element methodology to estimate the vibration analysis of functionally graded rotating annular plate. An extensive study is carried out using a finite element analysis. The Natural frequencies of annular plates with different boundary conditions are derived by the present approach and their effect on natural frequency is discussed.

INTRODUCTION

Introduction of functionally graded material (FGMs)

FGMs are defined as an anisotropic material whose physical properties vary throughout the volume, either randomly or strategically, to achieve desired characteristics or functionality. FGM are special composites usually made of a mixture of ceramic and metal and thus it can resist high temperature conditions while maintaining toughness, the composition of the FGM changes from a ceramic surface to a metal with a desired variation of the volume fraction. It is heterogeneous material and is defined for those objects with, and/or multiple material objects having clear material zone. The ceramic constituent provides a temperature resistance because it has low thermal conductivity and on the other hand the metal constituent assists to prevent fracture due to thermal stresses. Thus the FGM can be used to avoid interfacial stress concentrations appeared in laminated structures. Functionally graded materials are new innovative multifunctional material in which volume fractions of the reinforcement phases deviate. Furthermore the functionally graded material allows the certain more and numerous properties without any feeble interface. This new idea of materials hinges on mechanics and materials science due to integration of the structural and material importance into the final design of various mechanical and structural components. however steady change of material properties can be varied according to need in various applications and service conditions. Compared with the analysis of functionally graded plates and functionally graded spheres as well as functionally graded cylindrical shells the study of functionally graded circular and annular plates is very limited in number.

History of Functionally Graded Materials

First functionally graded material was introduced in 1984 in the course of a space project plane in japan by Japanese  marerial scientists. A various blending of materials which is used to serve the purpose of a large thermal resistance which is capable to bear a surface temperature of 1727 degree centigrade and a temperature gradient of 727 degree centigrade of a section 10 mm. recently functionally graded materials concept has become more popular in all over the world. there is a cooperative research center Transregio (SFB Transregio) funded since 2006 in order to explore the potential of grading mono-materials, such as aluminium, polypropylene and steel by using thermo mechanically coupled production processes.

Application of FGMs

There are many areas of application for FGM. The concept is to make a composite material by varying the microstructure from one material to another material with a specific gradient. This enables the material to have the best of both materials. If it is for thermal, or corrosive resistance or malleability and toughness both strengths of the material may be used to avoid corrosion, fatigue, fracture and stress corrosion cracking. The transition between the two materials can usually be approximated by means of a power series. The aircraft and aerospace industry and the computer circuit industry are very interested in the possibility of materials that can withstand very high thermal gradients. This is normally achieved by using a ceramic layer connected with a metallic layer. Advanced Materials and Processes Strategic Research Programme (AMPSRA) have done analysis on producing a thermal barrier coating using ZrO2 and NiCoCrAly. Their results have proved successful but no results of the analytical model are published. In engineering field it is used such as Turbine blade, helicopter blade, beams, bridges, column, shaft, rotor, nuclear reactor, cutting tool, machine parts and engine components, which require corrosion and, wear resistance, mechanical shock etc. Aerospace field such as Aerospace skins, space planes, nuclear reactors, space structures, nuclear reactors, insulations for cooling structures, Adaptive structures, Rocket engine components, Vibration control. In Electronics field for making graded band semiconductor, sensor, circuits etc. and also for making optical fiber, lens, Building materials, Sports good, Car body, Heat Exchanger, Reactor Vessel, Heat Pipe Nuclear weapons, Missile, High Speed Jet and Rocket, Arms and ammunitions etc. The rendition of the term that relates to the additive fabrication processes has its origins at the RMRG (Rapid Manufacturing Research Group) at Loughborough University in the United Kingdom. The term forms a part of a descriptive taxonomy of terms relating directly to various particulars relating to the additive CAD-CAM manufacturing processes, originally established as a part of the research conducted by architect Thomas Modeen into the application of the aforementioned techniques in the context of architecture.

Review of Relevant Literatures

Vibration is one of the Important phenomena in engineering application, it is particularly very

important item in the design of modern high speed engines such as turbo machinery.spinning disk is used in many application as for circular sawblades, turbine rotars, brake systems, fans, flywheels, gears, grinding wheels, precision gyroscopes, computer storage devices. Along with the dynamics of spinning disks is also a very important research ares.due to increase in research activity functionally graded material of rotating disk is frequently used since it has excellent properties. Many researchers have studied the dynamic behavior of bladed disks using various approaches . Rzadkowski has used the Ritz method to formulate the frequeny equation for a very general bladed disk model and calculate the natural frequencies and maximum stress level of a mistuned system. Yuan and Dickinson proposed a technique of introducing artificial springs between the components of a system which has straight and curved beams and which is based on the Ritz procedure. Cheng and Nicolas also find the free vibration of a cylindrical shell and circular plate system by using the artificial spring technique. Liew and Lam and Lam et al studies the free vibration of isotropic,anisotropic or composite plates of various Shapes and free vibration of annular composite plates and sectorial plates subjected to certain complicating effects by using orthogonal polynomials is given by Kim and Dickinson.

vibration theory of plates

The equations governing the motion of plates are simpler than those for general three-dimensional objects because one of the dimensions of a plate is much smaller than the other two. This suggests that a two-dimensional plate theory will give an excellent approximation to the actual three dimensional motion of a plate-like object, and indeed that is found to be true. There are several theories that have been developed to describe the motion of plates. The most commonly used are the Kirchhoff-plate theory and the Mindlin-Reissner theory. Solutions to the governing equations predicted by these theories can give us insight into the behavior of plate-like objects both under free and forced conditions. This includes the propagation of waves and the study of standing Waves and vibration modes in plates. In solid mechanics, a plate is often modelled as a two dimensional elastic body whose potential energy depends on how it is bent from a planar configuration, rather than how it is stretched (which is instead  the case for a membrance such as a durmhead )

MATHEMATICAL DEMONSTRATION

An elastic member under tension can support transverse vibrations.the properties of an idealized body can be modelled by the vibration of  circular  membrane of uniform thickness attached to a rigid frame. Due to the phenomenon of resonance, at certain vibration frequencies, frequencies, the membrane can store vibrational energy, the surface moving in a characteristic pattern of standing waves. This is called a normal mode. A membrane has an infinite number of these normal mode, starting with a lowest frequency one called the fundamental mode. plate have a wide variety of application in engineering science such as in construction, civil engineering mechanical  engineering aerospace industries, marine engineering, off-shore structures etc. So to have a satisfactory design which full fills the required purpose, it is essential to carry out thorough investigation of different aspects of plate behaviour.

plates can be classified into different categories depending on various characteristics, such as,

shape of cross-section (rectangular, box, channel, I-section, T-section etc.), geometric profile along the longitudinal dimension (uniform and non-uniform), boundary conditions etc. plates are associated with some boundary conditions include the following: clamped (C), simply supported (S) and free (F). Combinations of these  gives different classical boundary conditions, such as, clamped-clamped (CC), simply supported (SS), clamped-simply supported (CS) and clamped-free (CF).

RESULT AND DISCUSION

The study in this paper is conducted with an objective to investigate the vibration behaviour of functionally graded rotating plate and also to study the influence of various flexural boundary condition, material property variations on the frequency response. the material properties along the thickness direction is consider in this analysis.. the flexural boundary conditions made up of combinations of simply supported (S), clamped(i.e fixed) (C) and free (F)namely FF, and CC are considered. The results which are non-dimensional frequency response curve are plotted for these boundary conditions with variation of material roperty (i.e. elastic modulus and density) which vary with the volume fraction of functionally graded material. The effect of variation in thickness of the plate on frequency response has been considered as well.

Validation study

To show the validation and accuracy of the present approach, some example problems with different ratios of inner-to-outer radius, rotational speeds and boundary conditions are analysed to calculate their natural frequencies. In the present approach results are obtained for free-free and fixed-fixed boundary condition of annular plate made of functionally graded material.

| Ro/Ri=2.5 |  |  |  | Ro/Ri=5 |  |  |  | Ro/Ri=10 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Free-free | 6.94 | 7.76 | 8.84 |  | 8.98 | 9.05 | 9.11 | 11.23 | 12.45 | 13.67 |
| Fixed-fixed | 39.97 | 40.30 | 41.56 |  | 42.80 | 43.34 | 44.09 | 49.20 | 50.67 | 53.68 |

Conclusion

The vibrations analysis of functionally graded rotating plate is Presented. The fundamental frequencies of system are taken from literature review. By using governing differential equations of motion is derived and governing equation is solved by substitution technique with successive relaxation scheme present. The results are presented in the non-dimensional characteristics curve (frequency-response plot). The validation of the obtained result is done by the prior published paper. The frequency response curves for various combinations of material, and boundary conditions are obtained. And it is seen that the frequency increases for increasing rotational speed, outer inner radius ratio and also thickness. Finally, it can be concluded that the present work can be used for vibration analysis of the functionally graded rotating plate for different end conditions and different loading pattern.

REFERENCE

H1 CHARLES W. BERT, TAPAN K. PAUL,FAILURE ANALYSIS OF ROTATING DISKS, Inl. J. Soli & Stmcrures Vol. 32, No. S/9, pp. 1307-1318, 1995.

11 Ting Nung Shiau , Vibration and optimum design of rotating laminated blades, Composites: Part B 27B (1996) 173-183.

131 Timoshenko, S.P.and woinowsky-kreiger,S.,(1959), "theory of Elastic plates and shells", McGraw-Hill, New York.

[4] T.TOMIOKA, Y.KOBAYASHI AND G.YAMADA, ANALYSIS OF FREE VIBRATION OF ROTATING DISK-BLADE COUPLED SYSTEMS BY USING ARTIFICIAL SPRINGS AND ORTHOGONAL POLYNOMIALS, Journal of Sound and Vibration (1996) 191(1),52-73.

[51 M. P. MIGNOLET, FREE VIBRATION OF FLEXIBLE ROTATING discs, Journal of Sound and Vibration (1996) 196(5),537-577.

[6] U. GOVEN, ELASTIC-PLASTIC STRESS DISTRIBUTION IN A ROTATING HYPERBOLIC DISK WITH RIGID INCLUSION, Int. J. Mech. Sci. Vol. 40, No. 1, pp. 97 109,1998.

[7] Rajeev Jain, Rotating anisotropic disc of uniform strength, International Journal of Mechanical Sciences 41 (1999) 639Ð648.

[8] G. Venkateswara Rao, A FINITE ELEMENT FREE VIBRATION ANALYSIS OF A THERMALLY STRESSED SPINNING PLATE, Computers & Structures Vol. 59, No. 2. pp. 377385, 1996.

[9] L. H. You , J.J. Zhang, Elastic-plastic stresses in a rotating solid disk, International Journal of Mechanical Sciences 41 (1999) 2695282.

[10] Guido Dhondt, The effect of the geometry and the load level on the dynamic failure of rotating disks, International Journal of Solids and Structures 36(1999) 789-812.

[11] Chomg-Fuh Liu, Axisymmetric vibration analysis of rotating annular plates by a 3D finite Clement, International Journal of Solids and Structures 37 (2000) 5813-5827

[12] Vibration 298 (2006) 307–318. (24) Hassan Eid, George G. Adams, Critical speeds and the response of a spinning disk to